观海® TT

产品特性FEATURES

•

推荐使用APPLICATIONS

•

典型参数 Typical Properties

| 性能Properties | 测试标准Testmethod | 参数Value | 单位Units |
| --- | --- | --- | --- |
| 拉伸强度 TensileStrength | ISO527 | 70 | MPa |
| 伸长率 Elongationatbreak | ISO527 | 5 | % |
| 弯曲强度 FlexuralStrength | ISO178 | 95 | MPa |
| 弯曲模量 FlexuralModulus | ISO178 | 5500 | MPa |
| 悬臂梁缺口冲击强度 ImpactStrength,Charpynotched | ISO180 23℃ | 15 | KJ/m2 |
| 比重 Density | ISO1183 | 1.2 | g/cm3 |
| 收缩率 MoldShrinkage | ISO294-4(2mm) | 0.2 | (TD)% |

*典型性能基于常规生产经验，不应视作销售规格。

Typical properties are based on typical manufacturing experiences; they are not intended for sales specifications.

加工指南 Processing Guide

| 熔体温度MeltTemp | 200℃ |
| --- | --- |
| 模温MoldTemp | 60~80℃ |
| 后段Rear 中段 Center 前段 Front | 后段 160-200℃ / 中段 180-190℃ / 前段 190-200℃ |
| 注塑速度InjectionSpeed | 40%～80% |
| 背压Back Pressure | 0.3~1.0Mpa |
| 干燥条件DryingCondition | 90-110℃,2—4h |
| 加工上限温度 ProcessingTemp. | 260℃ |

以上数值仅供注塑机参考使用，可根据不同机型、不同模具以及产品要求做适当调整。

备注 Remarks

声明

典型值 这些数据仅作为典型值，不构成材料的规格限值或保证值。产品的性能受模具/机头设计、加工工艺条件以及着色情况的影响。除非另有特别说明，所有数据均来源于室温条件下对标准试样进行的测试。 通用免责声明 您对我们产品、技术协助及信息（无论是通过口头、书面还是生产评估方式提供）的使用及其目的，包括任何建议配方和推荐内容，均不受我方控制。因此，您有必要对我们的产品、技术协助、信息及建议进行测试，以确定其是否满足您的预期用途和应用需求。特定应用的分析必须至少包含测试，以便从技术、健康、安全和环保角度确定其适用性。我方未必进行过此类测试。 除非我方另行书面同意，否则所有产品均严格按照标准销售条款出售（可按需提供）。我方不对所提供的任何信息和技术协助进行担保或保证，如有变更，恕不另行通知。双方明确了解并同意，贵方将承担所有责任，并明确免除我方因使用我方产品、技术协助和信息而产生的任何侵权、合同或其他责任。此处未包含的任何声明或推荐均未经授权，对我方不具有约束力。此处任何信息均不得视为建议使用任何与相关材料或其用途的专利权相抵触的产品。此处信息不暗示或事实上授予任何专利许可。关于健康、安全和环保预防措施，在操作产品前，必须遵守相关的化学品安全技术说明书（MSDS）和产品标签。

Disclaimer

Typical Value These values are typical values only. They do not constitute a binding material specification or warranted values. Values may be affected by the design of the mold/die, the processing conditions and the coloring/pigmentation of the product. Unless specified to the contrary, the property values given have been established on standardized test specimens at room temperature. Global Disclaimer General The manner in which you use and the purpose to which you put and utilize our products, technical assistance and information (whether verbal, written or by way of production evaluations), including any suggested formulations and recommendations, are beyond our control. Therefore, it is imperative that you test our products, technical assistance, information and recommendations to determine to your own satisfaction whether they are suitable for your intended uses and applications. This application-specific analysis must at least include testing to determine suitability from a technical as well as health, safety, and environmental standpoint. Such testing has not necessarily been done by TingTao. Unless we otherwise agree in writing, all products are sold strictly pursuant to the terms of our standard conditions of sale, which are available upon request. All information and technical assistance is given without warranty or guarantee and is subject to change without notice. It is expressly understood and agreed that you assume and hereby expressly release us from all liability, in tort, contract or otherwise, incurred in connection with the use of our products, technical assistance, and information. Any statement or recommendation not contained herein is unauthorized and shall not bind us. Nothing herein shall be construed as a recommendation to use any product in conflict with any claim of any patent relative to any material or its use. No license is implied or in fact granted under the claims of any patent. With respect to health, safety, and environmental precautions, the relevant Material Safety Data Sheets (MSDS) and product labels must be observed prior to working with our products.